1. PLANT MIX SURFACING MIX DESIGN TRANSFERS [401] (Added 4-24-25)

Submit a mix design in accordance with Section 401. The following mix design considerations will be made for contracts requiring binder meeting the requirements of AASHTO M 332.

For contracts specifying 58V-34 or 58H-34, an unexpired, verified and approved PG 70-28 mix design may be considered for transfer provided it is modified to use the contract specified M 332 MSCR binder.

For contracts specifying 58H-34, an unexpired, verified and approved PG 64-28 or 58V-34 mix design may be considered for transfer provided it is modified to use the contract specified M 332 MSCR binder.

For contracts specifying 58S-34, an unexpired, verified and approved design utilizing the binder grades above will be considered for transfer provided it is modified to use the contract specified M 332 MSCR binder.

The contract specified binder will not be changed and not all mix designs described above may be eligible for transfer. Submit form MDT-MAT-009 to document the original mix design change of binder grade to the contract specified M 332 binder grade.